## Slide 1: MIT 3.071 Amorphous Materials 1: Fundamentals of the Amorphous State
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: Contact Information
Juejun (JJ) Hu, Rm 13-4054
hujuejun@mit.edu
Ph: (302) 766-3083
Research interests
  We work with light
  Optics & photonics
  Novel optical materials (including amorphous materials)
  Optical sensing, imaging, communications, solar energy, and many other topics related to light

## Slide 3: References
Fundamentals of Inorganic Glasses
  Arun Varshneya, Academic Press (1994)
  Arun Varshneya, John Mauro, Third Edition (2019)
  Google Books, Google Books
Introduction to Glass Science and Technology
  James E. Shelby, Royal Society of Chemistry (2005)
  RSC Publishing
Glass Science, 2nd Edition
  Robert H. Doremus, Wiley (1994)
Springer Handbook of Glass
  J. D. Musgraves, J. Hu, L. Calvez (Eds.), Springer (2020)

## Slide 4: Class organization
Modules
  Lectures: MW 1-2:30
  In-class demos (including a joint session with the MIT Glass Lab)
  Individual project meetings
  Final project presentation
  Pick-your-own-topic lectures
Canvas site
  Announcements, lecture slides, assignments, and solutions will be posted online
  Spring 2024 Canvas Link

## Slide 5: Pick-your-own-topic lectures
You pick the topic, and I present
  Submit your topic proposal by Apr. 15
  Topics must be relevant to amorphous materials
  Think about depth and breath
  If there are more topics proposed than lecture slots available, we will set up a voting system
You
JJ

## Slide 6: Grading policy
Homework assignments: 30%
  Three PSets
  Discussions are allowed and encouraged; but you are supposed to complete the assignments independently
Design review project: 70%
  Project proposal: 20%
  Term paper: 30%
  Final presentation: 20%

## Slide 7: Important dates
Mar. 20 project proposal due
  Page limit: 4 (including figures, tables, and references); Font: Times New Roman 12; Page format: letter size with 1 inch margin
  Motivation and significance; Brief review of state-of-the-art; Proposed technical approach; Anticipated outcome
  1 executive summary slide
May 8 project presentation
  Time limit and format: TBD

## Slide 8: Important dates
May 13 term paper due
  Page limit: 8 (including figures, tables, and references); Font: Times New Roman 12; Page format: letter size with 1 inch margin
  Motivation and significance; Current state-of-the-art; Research methodology; Results and discussion; Conclusions
Document templates are posted on Canvas

## Slide 9: Project topic examples
Glass box cracks at 1,353 feet above: is it still safe?
Can we make smart phones smarter with built-in photonics?
Opt. Express 22, 15473 (2014)
Where is my metallic glass cased iPhone?
Are smart windows technologically and economically viable?

## Slide 10: DMSE Breaker Space
Desktop Scanning Electron Microscope
Benchtop X-ray
Diffractometer
Tensile, Compression, and Flexure Testing
Material exploration and characterization lab allowing undergrads direct access to powerful instruments, including…
https://dmse.mit.edu/education/dmse-breakerspace/

## Slide 11: Evaluation criteria
Proposals and papers
  Intellectual merits (75%): soundness, depth, thoroughness, inventiveness
  Presentation (25%): logical coherence, clarity, conciseness
In-class presentation
  Timing (20%)
  Presentation (40%): logical coherence, clarity, conciseness
  Intellectual merits (40%): soundness, depth, thoroughness, inventiveness

## Slide 12: What is glass (amorphous solid)?
Solid matter
Amorphous solid
Glass
Silicate glass
“Glass” as we known it everyday

## Slide 15: What is glass (amorphous solid)?
Mechanical properties
  Brittle, fragile, stiff
Optical properties
  Transparent, translucent
“A room-temperature malleable glass” (As60Se40)
Video courtesy of IRradiance Glass Inc.

## Slide 16: What is glass (amorphous solid)?
Electrical properties
  Insulating
Chemical properties
  Durable, inert
NASA: Galileo Spacecraft found amorphous ice on moons of Jupiter
Man-made
  Obsidian (volcanic activity)
  Tektite (meteorite impact)
  Fulgurite (lightning strike)
Metallic glass

## Slide 17: The stone age… or the glass age?
“Obsidian is capable of producing an edge sharper than high quality steel razor blades…. What need could there be for a replacement material? The Aztecs didn't develop their use of metal because they couldn't see beyond obsidian.”
An Obsession with Obsidian

## Slide 18: Amorphous materials are ubiquitous
Glass cover
Camera lens
TFT display
Dielectrics
Circuit packaging
Metallic glass case
Phase change memory
Solid state battery
and many more…

## Slide 19
“The glassy state of matter: Its definition and ultimate fate,” J. Non-Cryst. Solids 471, 490 (2017)
Notes: Above TKS the average relaxation time of the SCL is shorter than the average crystal nucleation time, whereas for T < TKS the average nucleation time is shorter than the average relaxation time. Here TKS is the kinetic spinodal temperature. See Mauro et al. JNCS 2017.

## Slide 20: What is amorphous solid (glass)?
Solid matter
Amorphous solid
Glass
A metastable solid with no long-range atomic order
A metastable solid with no long-range atomic order and exhibiting a glass transition
Silicate glass
glass based on SiO2
“Glass” as we known it everyday

## Slide 21: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
metastable
E
Structure
Metastable glassy state
Thermodynamically stable crystalline state
Glasses are metastable with respect to their stable crystalline phase
Atoms can rearrange to form a more stable state given enough time and thermal energy

## Slide 22: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
no long-range atomic order
A2O3 crystal
A2O3 glass
Short-range order is preserved (AO3 triangles)
Long-range order is disrupted by changing bond angle (mainly) and bond length
Structure lacks symmetry and is usually isotropic
Zachariasen's Random Network Theory (1932)
Consider a fictitious A2O3 2-D compound:
Notes: Amorphous does not mean random

## Slide 23: Glass consists of a continuous atomic network
Absence of small angle scattering
  Continuous structure without micro-voids and micro-crystals
Broad diffraction peak
  Size of ordered region < 8 Å (Scherrer equation)
  Unit cell size of cristobalite: 7.1 Å
Glass is NOT a collection of extremely small crystals
J. Am. Cer. Soc. 21, 49-54 (1938)

## Slide 24: Random network model of silica glass (SiO2)
Nature 212, 1353 (1966)
Now in the Science Museum, London
Excellent agreement between XRD and ball-and-stick model constructed according to the random network model
Radial distribution function

## Slide 25: Direct atomic imaging of bilayer silica glass
O
Si
Si-O tetrahedron
O
O
O
2-D projection
Quartz crystal
Si

## Slide 26: Direct atomic imaging of bilayer silica glass
Sci. Rep. 3, 3482 (2013)
Nano Lett. 12, 1081-1086 (2012)
STEM images of 2-D silica crystal and glass

## Slide 27: Glass formation from liquid
V, H
T
Tm
When the system is kept in thermal equilibrium:
First-order liquid-solid phase transition
Discontinuity of extensive thermo-dynamic parameters (e.g., V and H)
Reversible process
Liquid
Crystal
Melting / solidification
Notes: The enthalpy plot is generic but the V-T is not: note volume anomaly in silica glass

## Slide 28: Glass formation from liquid
T
Tm
Supercooled liquid
Glass transition
Glass
Crystal
Tf
Supercooled liquid transforms to the glassy state when crystallization is kinetically suppressed
Extensive variables remain continuous during glass transition
The glassy state is different from super-cooled liquid
Tf : Fictive temperature
Liquid
V, H
Notes: Slope change between liquid and solid: heat capacity or thermal expansion coefficient change

## Slide 29: Glass formation from liquid
V, H
T
Tm
Supercooled liquid
Liquid
Increasing
cooling rate
3
2
1
Glasses obtained at different cooling rates have different structures
With increasing cooling rate:
V1 < V2 < V3
Free volume increases
H1 < H2 < H3
Configurational entropy increases
Tf,1 < Tf,2 < Tf,3

## Slide 30: Glass formation from liquid
T
Tm
Supercooled liquid
Liquid
The heating curve never retraces the cooling curve during glass transition due to structural relaxation
V, H

## Slide 31: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
Liquid: atoms do not have fixed positions; bonding constraints relax as temperature rises
Crystal: atoms arranged with both short range and long range order
Glass: atoms arranged with short range order but lack long range order
Solidification
Melting
Melt quenching
Softening
Crystallization
Amorphization (vitrification)

## Slide 32: What is amorphous solid (glass)?
A metastable solid with no long-range atomic order (and exhibiting glass transition)
Normalized distribution
Si-O-Si bond angle in fused silica
Si-O-Si bond-bending constraint is relaxed at the forming temperature of silica glass
Si-O-Si bond angle distribution in silica glass measured by XRD
J. Appl. Cryst. 2, 164 (1969)
144°: Si-O-Si bond angle in a-quartz

## Slide 33: Quantitative description of glass structure
Structural descriptions of amorphous materials are always statistical in nature
Pair distribution function (PDF): g(r)
  Consider an amorphous material with an average number density of atom given by:
  The number density of atoms at a distance r from an origin atom is given by
  When
  When
n : number of atoms V : material volume

## Slide 34: PDFs of ideal (hard sphere) crystals vs. glasses
g(r)
r
1st coordination shell
2nd coordination shell
g(r)
r
1
0

## Slide 35: Quantitative description of glass structure
Pair correlation function h(r)
Radial distribution function (RDF): J(r)
  J(r)dr gives the number of atoms located between r and r + dr away from the origin atom
  The area under the RDF curve gives the number of atoms
Reduced radial distribution function (rRDF): G(r)
Notes: Beware that different books may use different terminologies

## Slide 36: Summary
The amorphous state is metastable
Amorphous structures possess short-range order and lack long-range order
Amorphous materials can be obtained from liquid by melt quench
Melt quench is a continuous, irreversible process involving phase change
Glass properties depend on their thermal history
V, H
T
Tm
Supercooled liquid
Liquid
Glass
Crystal

## Slide 37: Crystalline vs. amorphous

## Slide 38: Crystalline vs. amorphous

## Slide 39: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 1 & 2
Introduction to Glass Science and Technology
  Ch. 1