## Slide 1: MIT 3.071 Amorphous Materials 3: Glass Forming Theories
Juejun (JJ) Hu
hujuejun@mit.edu

## Slide 2: After-class reading list
Fundamentals of Inorganic Glasses
  Ch. 3 (except Section 3.1.4 in the 1994 version)
Introduction to Glass Science and Technology
  Ch. 2
3.022 nucleation, precipitation growth and interface kinetics
Topological constraint theory
  M. Thorpe, “Continuous deformations in random networks”
  J. Mauro, “Topological constraint theory of glass”

## Slide 3: Glass formation from liquid
T
Tm
Supercooled liquid
Glass transition
Glass
Crystal
Tf
Supercooling of liquid and suppression of crystallization
Glass transition: from supercooled liquid to the glassy state
Glass forming ability: the structural origin
Liquid
V, H

## Slide 4: Glass forming theories
The kinetic theory
  Nucleation and growth
  “All liquids can be vitrified provided that the rate of cooling is fast enough to avoid crystallization.”
Laboratory glass transition
  Potential energy landscape
Structural theories
  Zachariasen’s rules
  Topological constraint theory

## Slide 5: Crystallization is the opposite of glass formation
Crystallized
Amorphous
Suspended Changes in Nature, Popular Science 83 (1913).

## Slide 6: Thermodynamics of nucleation
G
Liquid
Crystal
Tm
T
When T < Tm,
Driving force for nucleation

## Slide 7: Thermodynamics of nucleation
Surface energy contribution
Energy barrier for nucleation
Homogeneous nucleation
Heterogeneous nucleation
DG
Size
W

## Slide 8: Kinetics of nucleation
DG
Size
W
Nucleation rate:

## Slide 9: Kinetics of growth
Atom
Flux into the nucleus:
Flux out of the nucleus:
Nucleus

## Slide 10: Kinetics of growth
Atom
Net diffusion flux:
Nucleus

## Slide 11: Crystal nucleation and growth
Metastable zone of supercooling
Tm
Driving force: supercooling
Both processes are thermally activated
Supercooling
Crystallization

## Slide 12: Time-temperature-transformation diagram
Critical cooling rate Rc
R. Busch, JOM 52, 39-42 (2000)
Driving force (supercooling) limited
Diffusion limited

## Slide 13: Critical cooling rate and glass formation
Technique | Typical cooling rate (°C/s)
Air quench | 1-10
Liquid quench | 103
Droplet spray | 102-104
Melt spinning | 105-108
Selective laser melting | 106-108
Vapor deposition | Up to 1014
Material | Critical cooling rate (°C/s)
Silica | 9 × 10-6
GeO2 | 3 × 10-3
Na2O·2SiO2 | 6 × 10-3
Salol | 10
Water | 107
Vitreloy-1 | 1
Typical metal | 109
Silver | 1010
Maximum glass sample thickness:
a : thermal diffusivity

## Slide 14: Glass formation from liquid
V, H
T
Tm
Supercooled liquid
Liquid
Increasing
cooling rate
3
2
1
Glasses obtained at different cooling rates have different structures
With infinitely slow cooling, the ideal glass state is obtained

## Slide 15: Potential energy landscape (PEL)
The metastable glassy state
E
Structure
Metastable glassy state
Thermodynamically stable crystalline state

## Slide 16: Potential energy landscape (PEL)
PE
Atomic coordinates r1, r2, … r3N
Crystal
Ideal glass
Laboratory glass states

## Slide 17: Laboratory glass transition
Liquid: ergodic
Glass: nonergodic, confined to a few local minima
Inter-valley transition time t :
Liquid
Glass
B : barrier height
n : attempt frequency

## Slide 18
Glass formers
Network modifiers
Intermediates
Glass former: high valence state, covalent bonding with O
Modifier: low valence state, ionic bonding with O
Notes: The traditional classifications of glass former and modifiers are based on quenching from glass forming liquids

## Slide 19: Zachariasen’s rules
Rules for glass formation in an oxide AmOn
An oxygen atom is linked to no more than two atoms of A
The oxygen coordination around A is small, say 3 or 4
  Open structures with covalent bonds
  Small energy difference between glassy and crystalline states
The cation polyhedra share corners, not edges, not faces
  Maximize structure geometric flexibility
At least three corners are shared
  Formation of 3-D network structures
Only applies to most (not all!) oxide glasses
Highlights the importance of network topology

## Slide 20: Classification of glass network topology
Floppy / flexible
Underconstrained
  # (constraints) < # (DOF)
  Low barrier against crystallization
Isostatic
Critically constrained
  # (constraints) = # (DOF)
  Optimal for glass formation
Stressed rigid
Overconstrained
  # (constraints) > # (DOF)
  Crystalline clusters (nuclei) readily form and percolate
PE
r1, r2, … r3N
PE
r1, r2, … r3N
PE
r1, r2, … r3N

## Slide 21: Number of constraints
Denote the atom coordination number as r
Bond stretching constraint:
Bond bending constraint:
  One bond angle is defined when r = 2
  Orientation of each additional bond is specified by two angles
Total constraint number:
Mean coordination number:

## Slide 22: Isostatic condition / rigidity percolation threshold
Total number of degrees of freedom:
Isostatic condition:
Examples:
  GexSe1-x
  AsxS1-x
  SixO1-x
Why oxides and chalcogenides make good glasses?
Phillips' “magic”
coordination number
Notes: Two-fold coordinated oxygen and chalcogen atoms easily create long, spaghetti-like molecular chains that easily entangle and prevent crystallization. Additional three-fold or four-fold coordinated atoms provide cross-linking sites to form a 3-D continuous network.

## Slide 23: Temperature-dependent constraints
The constraint number should be evaluated at the glass forming temperature (rather than room temperature)
  Silica glass SixO1-x
  Bond stretching
  O-Si-O bond angle
  Isostatic condition
Normalized distribution
Si-O-Si bond angle in silica glass
  SiO2
Notes: Tg for silica > 1,100 C

## Slide 24: Temperature-dependent constraints
Each type of constraint is associated with an onset temperature above which the constraint vanishes
  “Topological constraint theory of glass,” ACerS Bull. 90, 31-37 (2011)
Notes: Basic protocols of applying topological constraint theory for glass property prediction: 1) structural determination; 2) calculate constraints as a function of glass composition and temperature; 3) determine entropy associated with the network structure; 4) use statistical mechanics (e.g. Gibb-Adams theory) to correlate entropy with macroscopic properties.

## Slide 25: Enumeration of constraint number
Bond stretching constraints (coordination number):
8-N rule: applies to most covalently bonded nonmetals (O, S, Se, P, As, Si, etc.)
Exceptions: heavy elements (e.g. Te, Sb), boron anomaly
Bond bending constraints:
Glasses with low forming temperature:
Atomic modeling or experimental characterization required to ascertain the number of active bond bending constraints

## Slide 26: Property dependence on network rigidity
Many glass properties exhibit extrema or kinks at the rigidity percolation threshold
J. Non-Cryst. Sol. 185, 289-296 (1995).

## Slide 27: Measuring glass forming ability
Figure of merit (FOM):
Tx : crystallization temperature
Tg : glass transition temperature
T
CP
Heat capacity
Tg
Tg is dependent on measurement method and thermal history
Alternative FOM:
Hruby coefficient

## Slide 28: Summary
Kinetic theory of glass formation
  Driving force and energy barrier for nucleation and growth
  Temperature dependence of nucleation and growth rates
  T-T-T diagram and critical cooling rate
Laboratory glass transition
  Potential energy landscape
  Ergodicity breakdown: laboratory glass transition
  Path dependence of glass structure
Glass network topology theories
  Zachariasen’s rules
  Topological constraint theory
Parameters characterizing glass forming ability (GFA)